## Slide 1
1. Part analysis
2. Runner analysis
3. Runner Injection condition
4. Fill time
5. Fill time (animation)
6. Flow front temperature
7. Temperature(animation)
8. Filling end pressure
9. Pressure(animation)
Job for: 100112.19-13_Halter
Date：2018.07.28
Catalog:
10. Injection location pressure: XY figure
11. Clamp force: XY figure
12. Weld line
13. Air traps
14. Shrinkage estimation
15. X Component deflection
16. Y Component deflection
17. Z Component deflection

## Slide 2
Product structure analysis
* Part name : EG20181166
- Gate thickness: 3.0（mm）
- Average wall thickness : 2.5（mm）
* Part information:
- Weight: 33.34g
- Cavity no. : 1
- Spec.: 86*81*30（mm）
* Material info.：Delrin 100 NC010
- Manufacturer: DuPont Performance Polymers
- Brand: POM
- MFR: 2g/10min; Load: 2.16kg
- Material temp. : 210~220°C
- Mold temp.: 80~100°C
- Material melt temp.: 203°C
- Ejection temp.: 123°C

## Slide 3
Material introduction
Viscosity: The higher the viscosity, the greater the flow resistance and the difficulty of the flow. For the general thermoplastic, the viscosity is a function of the plastic composition, temperature, pressure and shear rate. As to the temperature effect, the viscosity of the thermoplastic is generally reduced with the temperature.
PVT (PVT Relationship): The specific volume or density of plastic is a function of phase state, temperature, pressure, etc. in general, it can be quantified by the state equation (state equation) or PVT equation. One but the model parameters are obtained by experiment, and the specific volume or density value of the plastic at a certain temperature pressure can be obtained.

## Slide 4
Runner Ø6
Gate Ø.1.5
Main runner Ø3.5
Runner system

## Slide 5
Fill Pattern
It is finish fill by 2.277s. The simulation results show that the current gate condition can meet the molding requirements.

## Slide 6
Play
Shift+F5
Part fill (animation)

## Slide 7
Flow front temperature
The flow front temperature distribution is based on the color distribution of the product and its corresponding value. The temperature is on the low side.

## Slide 8
The material flowing is bad when the pressure is 137.9MPA.
Pressure at V/P switchover

## Slide 9
Pressure
Max. pressure is 137.9MPA

## Slide 10
Clamp Force
Max clamp force is 10.57T.

## Slide 11
Air traps

## Slide 12
Weld lines are shown as picture.
Weld lines

## Slide 13
Volumetric Shrinkage

## Slide 14
Sink marks, index
There is visible shrinkage when it is over 0.025mm.

## Slide 15
The excessive cold here may affect the product's holding pressure.
As shown in the figure 6.03s:
Frozen layer fraction

## Slide 16
It is complete frozen in red, the circle area will be frozen at last.
As shown in the figure 58.29ss:
Frozen layer fraction

## Slide 17
Deflection, all effects: Deflection (Scale=1)

## Slide 18
Deflection, all effects: X Component (Scale=4)

## Slide 19
Deflection, all effects: Y Component (Scale=1)

## Slide 20
Deflection, all effects: Z Component (Scale=3)

## Slide 21
The fill pattern is ok.
Take care for venting design.
Weld line will be effect visible surface.(see page 12)
The needed max. pressure ：137.9MPA，the needed max. clamp force： 10.57T.
Deflection for reference.
Summarize: